Top Plate Strength Analysis

25 Jun, 2001  Tokoku

- Kerry’s design

Plate thickness = 15 or 20mm (window section thickness = 10mm)

Condition : 1atm, 293K

O-ring d = 270mm (round)

- Aluminum Property

|  | Density 103[kg/m3] | Young’s modulus [MPa] | Poisson ratio | Yield strength [MPa] |
| --- | --- | --- | --- | --- |
| Al2024 | 2.77 | 73.1*103 | 0.33 | 76-393 |
| Al6061 | 2.68 | 68.2*103 | 0.332 | 55-276 |
| Al7075 | 2.79 | 71.7*103 | -- | 103-503 |

- Result

t=15mm (window section t=10mm)

|  | Displacment dx[um] | Displacement dy[um] | Displacement dz[um] | Total disp. [um] | Max stress [MPa] |
| --- | --- | --- | --- | --- | --- |
| Al2024 | 5.41 | 7.62 | 99.04 | 99.07 | 11.02 |
| Al6061 | 5.82 | 8.17 | 106.16 | 106.19 | 11.01 |
| Al7075 | 5.24 | 7.76 | 100.83 | 100.85 | 11.16 |

t=20mm (window section t=10mm)

|  | Displacment dx[um] | Displacement dy[um] | Displacement dz[um] | Total disp. [um] | Max stress [MPa] |
| --- | --- | --- | --- | --- | --- |
| Al2024 | 4.21 | 5.13 | 52.27 | 52.32 | 7.31 |
| Al6061 | 4.53 | 5.50 | 56.03 | 56.10 | 7.31 |
| Al7075 | 4.10 | 5.25 | 53.04 | 53.10 | 7.39 |