Strength Analysis of the Top Plate and the Square Window

21 Jun, 2001  tokoku

TOP PLATE

- 630mm*310mm*t20mm, Al7075

- Condition

1atm, room temperature

- Boundary Position

edge of plate (edge of window hole are free)

- Displacement is ……

- Stress is weak enough

# WINDOW

- 223mm*133mm*t20mm, CaF2

- Condition

1atm, room temperature

- Boundary Position

Just put on the edge (10mm) of the top plate.

xy-direction are fixed at upper rim of window (like strong friction).

- Heat radiation is not considered.

- Displacement is no problem.

- Stress is no problem.